## Slide 1
mA current level operation of K2CsSb photocathode in DC-SRF-II gun
XIE Huamu on behalf the SRF team at PKU
Sep 17-19, 2024
EWPAA 2024

## Slide 2
Outline
Fabrication and Transport of K2CsSb photocathode
mA level operation of the K2CsSb photocathode in the DC-SRF gun
Emittance measurement
Summary

## Slide 3
Demand of K2CsSb photocathode
(Bruce Dunham, P3 Meeting 2018)
(Sonal Mistry, P3 Meeting 2018)
DC-SRF II
K-Cs-Sb
XFEL around the world
The spectral response of semiconductor photocathode
BERLinPro
DC-SRF-II gun at PKU

## Slide 4
K2CsSb photocathode deposition system
“Fast Cesiation” sequential deposition recipe, the total activation time cost less than 10 min. The QE keeps growing in the following days after activation.
Photocathode grown by co-evaporation method

## Slide 5
Dark lifetime in Deposition chamber and UHV suitcase
K2CsSb photocathode samples fabricated with Fast-cesiation recipe usually have a long dark lifetime in UHV environment.
In deposition chamber with a base vacuum of 4 ×10-11 Torr, the QE of K2CsSb photocathode sample was measured every 10 min, and remained at ~7% for more than 500 h.
We also tested the dark lifetime of K2CsSb photocathode in UHV suitcase, the QE showed no obvious decay for more than 3 weeks.

## Slide 6
Outline
Fabrication and Transport of K2CsSb photocathode
mA level operation of the K2CsSb photocathode in the DC-SRF gun
Emittance measurement
Summary

## Slide 7
DC-SRF-II parameters and layout
DC-SRF-II gun
2856MHz deflecting cavity
B magnet
Faraday cup
solenoid
corrector
YAG & FC
Parameters | Unit | Value
Beam energy | MeV | ~2
DC voltage | kV | 100
Dark current | pA | 100(CW)
Bunch charge | pC | 10-100
Bunch repetition rate | MHz | 1, 81.25
Normalized RMS emittance | mm.mrad | 0.28 @ 20 pC；0.43@ 50 pC；0.54 @ 100 pC
Laser wavelength | nm | 515

## Slide 8
CW operation of 100 μA
20231221#3 sample
20230914#3 sample
Extraction charge >5 C@5 mm

## Slide 9
QE evolution during beam experiments
As the result of cryogenic temperature effect and Schottky effect, the QE of K2CsSb photocathode in DC-SRF-II gun is usually ~20% of that in UHV suitcase at room temperature.
1st round-Decay from 0.9% to 0.2% within 3 days
2nd round-Decay from 1.0% to 0.2% within 7 days
Commissioning time | Pressure at the exit of DC-SRF-II[Pa] | Average lifetime[D]
#1-2023.03.31-06.28 | 2E-6 | ~3
#2-2023.08.28-09.28 | 8E-8 | ~7
#3-2023.12.29-2024.2.6 | 3E-8 | >20
3rd round
QE remained above 0.5% for more than 22 days
QE reduced by ~10% at room temperature after 2-week-operation
Still worked well after transferred into DC-SRF-II gun again

## Slide 10
Lifetime of the photocathode in DC-SRF gun
The photocathode in the suitcase has a quantum efficiency (QE) of about 5%. However, when inserted into the gun, the QE drops to approximately 1%. Once returned to the suitcase, the QE recovers to 5%.
QE is influenced by the vacuum conditions within the cavity, which are mainly determined by the cryogenic system. When the 2K system is closed, gases released from the cavity can poison the photocathode

## Slide 11
QE increasement during the beam experiment-observed in every beam experiment
11
20% Duty factor
Q ~ 60 pC
50% Duty factor
Q ~ 68 pC
CW
Q ~ 78 pC
CW
Q ~ 80 pC
Rise of photocurrent by 1MHz, 0.65W CW laser irradiation, Experiments on Jul 21, 2021
100 pC, 1 MHz CW operation, 6 Colum charge extracted from this cathode #202309
13 pC, 81.25 MHz CW operation on September, 2023
1mA CW, Rise of QE
Laser feedback added
Rise of QE
Laser power

## Slide 12
High current operation
CW operation at high average current---1 mA
QE increase due to laser power deposited on the plug
mA level CW beam extraction at a repetition rate of 81.25 MHz, QE kept growing during operation
5 mm laser spot for 1 mA operation, with a total extraction charge of 1.3 C

## Slide 13
CW operation of 2~3 mA
2mA CW operation
0914#3—1.4 C
3 mm laser spot for 2 and 3 mA operation, with a total extraction charge of 1.4 C and 0.9 C, respectively.
A continuous wave (CW) average current of 2 to 3 mA (12 to 40 pC at 81.25 MHz) has also been achieved in the DC-SRF-II gun.
3mA CW operation
0913#2—0.9 C

## Slide 14
1 mA beam acceleration with 2×9 cell accelerator
The beam line of DC-SRF gun and 2×9 cell accelerator
There are solenoid, dipole, Farady cup, ICT, YAG, CCD, deflecting cavity in the beam line. And the energy, bunch charge, emittance and the pulse length can be measured from the beamline.
The beam before(left) and after(right) the bending magnet

## Slide 15
Beam energy measurement
The control panel of the beam experiment
DC-SRF gun
2×9 cell accelerator
Duty Factor Measurement
The bunch repetition rate is set at 10 Hz, with a macro-pulse duration of 10 ms, and a duty factor of 10%.
Final test results indicate a beam energy of approximately 10.61 MeV, a duty factor of 10%, and an average current of 1 mA (limited by the amplifier's power) in the macropulse after the 2×9 cell accelerator.

## Slide 16
The challenge of the photocathode in cryogenic environment
How can the bialkali photocathode be utilized for high current/CW applications in a cryogenic environment(SRF gun)?
The QE of the bialkali photocathode should be maintained at a stable level. Previous investigations have shown that changes in the QE of the bialkali photocathode are significantly affected by temperature variations. This is only observed for bialikali photocathode, not observed for Cs2Te photocathode at cryogenic temperature, such as Cs2Te in SRF gun at HZDR, and Cs2Te in DC-SRF-I gun at PKU.
The bunch charge is changed during the operation, which is not good for the XFEL and other application. So the control loop of the laser is important to keep the bunch charge and the average current stable.
Other ways to keep the QE of the bialkali photocathode stable at cryogenic temperature?
For high current application, it is better to keep the temperature of the bialkali photocathode at RT more than cryogenic temperature. For example, with flowing water(bialkali photocathode in 112 MHz QWR SRF gun at BNL) or back illuminating heating laser.

## Slide 17
Outline
Fabrication and Transport of K2CsSb photocathode
mA level operation of the K2CsSb photocathode in the DC-SRF gun
Emittance measurement
Summary

## Slide 18
Emittance measured in the DC-SRF gun
Electron energy(Ek) 2.23 MeV
Bunch charge(Q) 1.6 fC
Pulse length (FWHM) 1 ps
Laser spot (σ) 0.30 mm
Transverse distribution of the electron pulse after multipole field calibration
transverse distribution of the laser spot
Emittance measurement by slit scanning
The normalized emittance: 0.13 mm-mrad;
The intrinsic emittance: 0.42 mm-mrad/mm@30K, 515 nm.
Compared to 0.5 mm.mrad/mm measured at room temperature in 100 kV HV DC gun.
Preliminary results, will be measured further!
Parameters of the experiment:

## Slide 19
Summary
The continuous wave (CW) operation of the photocathode can be sustained for up to 16 hours at an average current of 0.1 mA (100 pC, 1 MHz), with average currents between 1 and 3 mA (CW, 81.25 MHz) having been successfully demonstrated in the DC-SRF-II gun.
To achieve high average current applications, additional research is required to optimize the performance of bialkali photocathodes operating at cryogenic temperatures. The quantum efficiency (QE) of the photocathode should be maintained at a constant value by regulating the temperature around room temperature (RT) through controlled water flow. This regulation is essential for stabilizing the bunch charge of the electron pulse; otherwise, laser feedback mechanisms must be employed.
The intrinsic emittance of the K2CsSb photocathode is approximately 0.5 mm·mrad/mm at room temperature as measured in the high voltage (HV) DC gun, and about 0.4 mm·mrad/mm at 30 K, measured in the DC-SRF gun (preliminary results).
The photocathode has been effectively operated in the DC-SRF gun, demonstrating reliable performance within the cryogenic environment. Following insertion into the gun, the QE of the photocathode stabilized near 0.6~1%. During the CW beam experimentation, the QE gradually increased to 2 to 3 times this initial value. Notably, when the cold cathode is extracted back to RT conditions, its QE can return to the original value exceeding 5%.
Furthermore, the lifetime of the bialkali photocathode is significantly affected by the vacuum conditions within the gun; a low 10⁻⁸ Pa pressure is required to ensure prolonged operation within the gun.

## Slide 20
Lab of Superconducting Radio Frequency Accelerator
Thanks for your attention!