## Slide 1: Promoting Epitaxy in Alkali Antimonides Jared Maxson Cornell University EWPAA, Sep 18 2024 HZDR

## Slide 2: Overview
The phrase “promoting epitaxy” has two interpretations:
Encouraging the conditions for epitaxy during material growth
Popularizing/advertising the benefits of epitaxial cathodes
I will try to do both.

## Slide 3: Acknowledgements
The data in this talk is the result of the work of a large team. I take credit for very little of it!
Cornell: C. Pennington, E. M. Echeverria, C. Parzyck, J.K. Nangoi, T. Wu, W. DeBenedetti, K. Shen, D. Schlom, M. Hines, T. Arias, H. Paik, C. Hu
Brookhaven National Lab: M. Gaowei, , K. Evans-Lutterodt, K. P. Mondal
U. Salerno: A. Galdi
U. Vienna: T. Juffmann
Arizona State: S. Karkare, P. Saha
SLAC: J. Smedley
Leiden University: S.J. van der Molen, W.G. Stam
IBM: R.M. Tromp
This work was funded in part by DOE Basic Energy Sciences, as part of a grant to study photocathodes for LCLS-II-HE, and by the NSF Center for Bright Beams.
Special thanks to my “Gurus”:
A. Galdi (MBE, RHEED)
J. Smedley + M. Gaowei (X-ray characterization

## Slide 4: The meaning of “epitaxy”
Epitaxy: using a crystalline substrate to seed the growth of (at least approximately) lattice-matched films.
An epitaxial films has only one or few definite lattice relationships between the substrate and film.
Often the goal is a single relationship between substrate and film, approaching single crystal growth. “Lattice matching”.
Google Etymology
Google Ngram Viewer
year
now
1991
1920
Usage in Books

## Slide 5: Benefits of Epitaxy
Epitaxial films can be near-atomically smooth.
Note: Limited experimental demos of these so far (hard to control!), but these rules are very fundamental.
MTE from “chemical” roughness
Karkare and Bazarov. Phys. Rev. Appl., 4:024015 (2015)
G. S. Gevorkyan et al.,
Phys. Rev. Accel. Beams 21, 093401 (2018)
Surface potential
variation
Applied field
MTE from physical roughness
Feng et al., J. Appl. Phys. 121, 044904 (2017) (see references therein)
Applied field
wavelength
Fourier Amplitude
Why care?

## Slide 6: Benefits of Epitaxy
Epitaxial films can be near-atomically smooth.
Example: Cs1Sb (See A. Galdi’s talk)
  Grown on lattice matched substrates (3C-SiC and Rutile TiO2)
  Not perfectly epitaxial: Rotational in-plane disorder w.r.t substrate.
  But nonetheless very flat, as measured by STM.
Note: Epitaxial films need not be smooth, and smooth films need not be epitaxial. It is a good place to start, though!
STM Measurements @ Cornell
Cs1Sb
looking down
[010]

## Slide 7: Benefits of Epitaxy
Epitaxial photocathodes have high QE even when very thin (fast)
Thin also means less scattering overall: perhaps closer to a “one step photoemitter?”
Single crystal Cs3Sb
(Explanation of how we know later)
Thin and high QE
As yet mysterious red enhancement! (work function? Less defect/impurity scattering?)
Parzyck et al., PRL 128, 114801 (2022)

## Slide 8: Benefits of Epitaxy
Epitaxial photocathodes have high QE even when very thin (fast)
Thin also means less scattering: perhaps closer to a “one step photoemitter?”
A series of Cs3Sb photocathodes grown on Si3N4, 3C-SiC, and Gr/4H-SiC also show very high QE at small thickness values.
W. G. Stam et al., APL Mater. 12, 061114 (2024)

## Slide 9: Benefits of Epitaxy
Single crystal substrates and smooth cathodes have another benefit: interference enhancement to QE:
1.3 um
~0.5 mm
Interference in the film thanks to substrate reflections
(SiC is ~transparent here). NB: Still fast!
Cs3Sb

## Slide 10: Some details on interference effects
We can model the interference effects quite well
  Use DFT for calculation of material properties (DoS, indices of refraction)
1.3 um SiC layer
0.3 um SiC layer
Fits to the data seem to yield reasonable thickness values!

## Slide 11: Benefits of Epitaxy
You can understand what you’ve grown!
  Examples: ARPES measurement compared to DFT
Epitaxial Cs3Sb on 3C-SiC
Parzyck et al., PRL 128, 114801 (2022)
Solid Curves:
DFT
Fiber-Textured
Cs1Sb1
Has a ~1-D band structure:
Even rotational disordered films show ARPES signals
Parzyck et. al, APL Mater. 11, 101125 (2023)

## Slide 12: Promote and Measure Epitaxy
Required: a structural probe on your growth system.
  Electron beams: Reflection high energy electron diffraction (RHEED)
mounted directly on growth chamber
Sensitive to sub-monolayer changes
What you’re often looking for:
Sign you’re on the right track…

## Slide 13: Promote and Measure Epitaxy
Required: a structural probe on your growth system.
  Electron beams: Reflection high energy electron diffraction (RHEED)
“Signs of roughness”
“At least it’s not amorphous!”
mounted directly on growth chamber
Sensitive to sub-monolayer changes
NB: RHEED is often, not always, qualitative.

## Slide 14: RHEED Examples
3C-SiC
substrate
Lineouts
Film
Parzyck et al., PRL 128, 114801 (2022)
Cs3Sb on 3C-SiC
Fiber textured
C. Pennington et al.,
arXiv:2407.12224
Cs3Sb on Gr/4H-SiC
(multiple orientations)

## Slide 15: Even more comprehensive: x-rays
Structure
Surface,
Structure,
roughness
Stoichiometry
“One stop shopping” at NSLS-II, ISR Beamline 4-ID
W. G. Stam et al., APL Mater. 12, 061114 (2024)

## Slide 16: X-ray studies on Cs3Sb on Gr/4H-SiC
2 nm
4 nm
10 nm
20 nm
0.7 nm roughness
0.38 nm roughness
0.84 nm roughness
X-ray Reflectivity
X-ray Fluorescence
Quantification of stoichiometry
In this case:
3.05:1 and 2.84:1 (Cs:Sb)
X-ray reflectivity models include surface
roughness (often RMS) as a fit parameter.
W. G. Stam et al., APL Mater. 12, 061114 (2024)

## Slide 17: X-ray studies on Cs3Sb on Gr/4H-SiC
X-rays: high coherence large scattering angle (compared to RHEED) allows you to see:
Laue fringes around Bragg peaks. Only appear if the crystal coherence length is at least comparable to the thickness.
  An indicator of high crystallinity
  Permits a fit of the film “coherent” thickness. Useful to compare this to XRR
High resolution view of strain relaxation: here, seen as peak splitting.
Laue Fringes in Cs3Sb
2 nm
4 nm
10 nm
20 nm
thickness
Strain relaxation
during growth
C. Pennington et al.,
arXiv:2407.12224

## Slide 18: X-ray vs Electron structural probes
Electrons (RHEED)
Much more “portable”: amenable to most growth systems
Extremely surface sensitive
Limited bulk sensitivity
Limited dynamic range and coherence
One or few probe techniques
Synchrotron X-rays
One stop shopping: many techniques
Very high structural resolution and dynamic range
Sensitive to whole film
Expensive and complex
Can be challenging to assess surface vs bulk contributions
Very complimentary!

## Slide 19: Summary and outlook
Epitaxy in the alkali antimonides has already unlocked new capabilities:
  Extremely flat surfaces, interference enhancement, high QE while very thin
It may lead to additional new capabilities
  Atomic scale layer engineering: heterostructures, polarized cathodes?
  MTEs dominated by band structure? (Particularly for thin cathodes)
X-ray and electron beam probe suites are vital for epitaxial growth: diffraction, spectroscopy, reflectivity, ….
Epitaxy enables precise understanding of materials properties and detailed comparison to ab-initio theory.