## Slide 1: OptaDOS Photoemission
Felix Mildner, Nicholas M. Harrison
18/09/2024
Interesting
The Good, The Bad and The Interesting

## Slide 2: The OptaDOS Program Suite
From Optics to Photoemission
Andrew J. Morris, R. J. Nicholls, C. J. Pickard and Jonathan R. Yates, The OptaDOS code, Comp. Phys. Comm. (2012).
R. J. Nicholls, A. J. Morris, C. J. Pickard and J. R. Yates, OptaDOS, Accepted for publication in Journal of Physics: Conf. Sers.
calculate DOS, PDOS and optical properties
Open source program
Photoemission part under active development
  release in the next version of OptaDOS
Dr Victor Chang Lee
Dr Bruno Camino

## Slide 3: The Model
Things to Consider
Things we can take into account:
    light intensity at each layer
    emission probability based on depth
      mean free path model
    K-resolved excitations + emissions
      explicit and detailed analysis of band contributions
    electronic transverse energy (weighted MTE)
    bulk region extension
      repeat innermost layer until minimum emission probability is reached
…
- reflection of layer 1
- Absorption of layer i

## Slide 4: The Model – cont.
Energies and Probabilities
E
Efermi
Eelectron – bound
Workfunction Ω
Eelectron - free
0
Evacuum
Optical Matrix Element (OME)
Fermi’s Golden Rule Type
MTE, weighted sum

## Slide 5: The Model – cont.
3-Step + 1-Step Model

## Slide 6: The Good
Detailed Contributions from Slab Layers
+---------------------- Bulk Approximation Slab Info ------------------------+
+ Number Bulk layers = 105 +
+ Vol. per layer = 11.2266 +
+ Total Volume = 1178.7943 +
+---- P_esc values for an electron with E = E_fermi and E_transverse = 0 ----+
+ Layer # 1 I_light = 0.529986E+00 P_esc = 0.469286E+00 +
+ Layer # 2 I_light = 0.517459E+00 P_esc = 0.426847E+00 +
+ Layer # 3 I_light = 0.499221E+00 P_esc = 0.388246E+00 +
+ ...... +
+ Layer # 103 I_light = 0.811068E-28 P_esc = 0.296874E-04 +
+ Layer # 104 I_light = 0.233806E-28 P_esc = 0.270026E-04 +
+ Layer # 105 I_light = 0.665977E-29 P_esc = 0.245607E-04 +
+----------------------------------------------------------------------------+
+----------------------------------------------------------------------------+ | Work Function 4.5519 eV Photon Energy 5.6600 eV | | Effective Work Function 4.5519 eV Electric Field 0.0000 V/A | | Final State : Bloch State | +----------------------------------------------------------------------------+ | Atom | Atom Order | Layer | Quantum Efficiency | | Cu 1 1 0.1181845906536724E-004 | | Cu 2 2 0.1663074525614247E-005 | | Cu 3 3 0.4194841801380124E-005 | | Cu 4 4 0.5232538050559572E-005 | | Cu 5 5 0.2940584626806248E-005 | | Cu 6 6 0.2580269949778397E-005 | | Cu 7 7 0.3055495698118412E-005 | | Cu 8 8 0.2217314887108183E-005 | | Bulk 0.1136553840413117E-004 | | Total Quantum Efficiency (electrons/photon): 0.4506811700886359E-004 | | Weighted Mean Transverse Energy (eV): 0.4243355184389246E+000 | +----------------------------------------------------------------------------+

## Slide 7: The Good – cont.
Detailed Contributions from Bands and K-points

## Slide 8: The Bad
Adapting a code made for bulk phase to slab geometries
dependence -> bad reference for slab
Cu(100) – 16 layers

## Slide 9: The Bad
Adapting a code made for bulk phase to slab geometries
Solved!
Cu(100) – 16 layers

## Slide 10: The Bad
Calculating Photoresponse of Supercells
pristine Cu(100) surface
possible application:
defective surfaces

## Slide 11: The Bad
Photoresponse of Supercells
possible solution: “unfolding” the bands
What is the right reference to unfold to?
  Would different reference systems give equal answers?
We also need to unfold the excitation probabilities
  need to write this piece of software, too
Others?
pristine Cu(100) surface
primitive cell
supercell

## Slide 12: The Interesting
Quantum Efficiency (QE) and Mean Transverse Energy (MTE)
OptaDOS MTE, weighted sum
ext. DS Model1 MTE
MTE (E) =
1. T. Vecchione, D. H. Dowell, W. Wan, J. Feng and H. A. Padmore, New York, 2013.

## Slide 13: The Interesting
Comparison to Experimental Data

## Slide 14: The Interesting
Comparison to Experimental Data

## Slide 15: The Interesting
Comparison to Experimental Data

## Slide 16: Summary + Future Work
OptaDOS Photoemission
K-resolved modelling of Photoemission
Very detailed analyses of contributions possible
currently working on:
    supercell representation
    weighted MTE calculation
  Future work:
  Adding other models into the code (e.g. P. Saha, et al.1).
  Add support for other DFT codes (Crystal, CP2K etc.).
1. P. Saha, O. Chubenko, J. Kevin Nangoi, T. Arias, E. Montgomery, S. Poddar, H. A. Padmore and S. Karkare, Journal of Applied Physics, 2023, 133.

## Slide 17: Acknowledgements
Prof Nicholas Harrison
and the other members of the
Computational Materials Science Group
CDT in ‘Advanced
Characterisation of Materials’
Dr Victor Chang Lee
Dr Bruno Camino
Dr Tim Noakes, Dr Lee Jones,
Chris Benjamin, Hugh Churn

## Slide 18: Thank you
OptaDOS Photoemission – The Good, The Bad and The Interesting
18/09/2024

## Slide 19: Cu(110) 16L slab
MTE near Threshold

## Slide 20: Cu(110) 16L slab
MTE near Threshold

## Slide 21: Cu(110) 16L slab
MTE near Threshold

## Slide 22: Cu(110) 16 layer slab

## Slide 23: Cu(110) 16 layer slab

## Slide 24: Cu(100) 16L slab
MTE near Threshold

## Slide 25: Cu(100) 16L slab
MTE near Threshold

## Slide 26: Cu(100) 16L slab
MTE near Threshold