## Slide 1
M. Herbert – J. Enders, M. Engart, M. Meier, J. Schulze, V. Wende, V. Winter
Activation studies for GaAs photocathodes at Photo-CATCH*
*Supported by BMBF (05H18RDRB1) and by DFG (GRK 2128 „AccelencE“, project-id 264883531)

## Slide 2: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
GaAs photocathode research at Photo-CATCH
Laser-induced photo-emission
High degree of spin-polarization possible
XHV required (~ 10-11 mbar)
used in DC HV guns
low- to medium-intensity electron beams
Challenge: high-intensity electron beams

## Slide 3: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Photoemission threshold for GaAs:
Eth > 5.52 eV or λ < 225 nm
Emission of polarized electrons from GaAs:
Eγ < 1.76 eV or λ > 705 nm

## Slide 4: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Photoemission threshold for GaAs:
Eth > 5.52 eV or λ < 225 nm
Emission of polarized electrons from GaAs:
Eγ < 1.76 eV or λ > 705 nm
Activation with NEA layer required to reduce work function!

## Slide 5: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Photoemission threshold for GaAs:
Eth > 5.52 eV or λ < 225 nm
Emission of polarized electrons from GaAs:
Eγ < 1.76 eV or λ > 705 nm
Activation with NEA layer required to reduce work function!
Co-Deposition (Co-De)

## Slide 6: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Photoemission threshold for GaAs:
Eth > 5.52 eV or λ < 225 nm
Main parameters: η0, τ, Q(τ)
Emission of polarized electrons from GaAs:
Eγ < 1.76 eV or λ > 705 nm
Activation with NEA layer required to reduce work function!
Surface layer decay

## Slide 7: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Photoemission threshold for GaAs:
Eth > 5.52 eV or λ < 225 nm
Main parameters: η0, τ, Q(τ)
Emission of polarized electrons from GaAs:
Eγ < 1.76 eV or λ > 705 nm
Activation with NEA layer required to reduce work function!
Surface layer decay
Dedicated activation studies
Outcome depends on operator input

## Slide 8: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Photo-CATCH

## Slide 9: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Photo-CATCH
Activation & Cleaning System

## Slide 10: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Activation Chamber
Activation & Cleaning System

## Slide 11: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Activation Chamber
Activation Setup

## Slide 12: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
QE scan setup
Measure QE distribution on photocathode surface
Dedicated laser beamline below activation chamber
Move laser-spot using piezo-electric mirror mount
Feedback position control via position-sensitive diode
Python-based

## Slide 13: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
QE scan setup
Implementation successful!

## Slide 14: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Adaptive Automated Activation using PyCAT
Python Cathode Activation Terminal
Advanced development following successful preliminary, timer-based tests
Based on automatic curve analysis (python code)
Parameters derived in real time during activation process

## Slide 15: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Adaptive Automated Activation
first tests successful!
Python Cathode Activation Terminal
data
smoothed
data
1st
derivative

## Slide 16: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Scheme 1
Scheme 2a
Scheme 2b
Li-enhanced activation
Goal: enhanced lifetime
Co-De with pulsed Li, based on previous study
Scheme 1: Cs + O2
Scheme 2a: Cs + O2 + Li, 5 pulses
Scheme 2b: Cs + O2 + Li, 8 pulses

## Slide 17: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Li-enhanced activation
QE & Lifetime measurements in activation chamber
Plaser = (50 ± 5) µW, λ = (785 ± 2) nm, Ubias = 100 V
5 types of activations:
  Scheme 1, no prior scheme 2
  Scheme 1, subsequent to scheme 2a
  Scheme 2a, subsequent to scheme 1
  Scheme 2b, subsequent to scheme 1
  Scheme 2b, subsequent to scheme 2b
Effect of Li on subsequent activations observed
Paper submitted

## Slide 18: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Li-enhanced activation
QE & Lifetime measurements in activation chamber
Plaser = (50 ± 5) µW, λ = (785 ± 2) nm, Ubias = 100 V
5 types of activations:
  Scheme 1, no prior scheme 2
  Scheme 1, subsequent to scheme 2a
  Scheme 2a, subsequent to scheme 1
  Scheme 2b, subsequent to scheme 1
  Scheme 2b, subsequent to scheme 2b
Effect of Li on subsequent activations observed
Significat increase in τ (up to factor 19) and Q(τ) (up to factor 16.5) observed!
Paper submitted

## Slide 19: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Li-enhanced activation (cont.)
Idea: simultaneous co-deposition of Li along with Cs and O2 instead of pulsed Li
First activation tests successful, QE comparable to Cs+O2 activation
BUT: first lifetime tests show no improvement
Additonal tests with higher Li dosage as well as comparison with pulsed scheme ongoing
Li on
Li off

## Slide 20: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Implementation of QE-scan setup
Development of automated activation scheme
Implementation of Li-enhanced activation yielding significant increase in lifetime
Benchmark automated vs manual activation
Test of Li Co-Deposition
Additional lifetime measurements of Li-enhanced activation
Conclusion

## Slide 21: Motivation – Experimental Setup – Automated Activation – Li-enhancement – Conclusion & Outlook
Additional studies with Li-enhanced activation
Further sophistication of automated activation scheme
Experiments with Photo-CATCH gun
High-polarization cathodes
Cryogenic gun development
Outlook

## Slide 22
AG Enders: Joachim Enders, Markus Engart, Maximilian Meier, Vincent Wende, Victor Winter Alumni: Tobias Eggert, Yuliya Fritzsche, Julian Schulze
S-DALINAC: Ruben Grewe, Felix Heyer Alumni: Manuel Steinhorst
IKP Electronics Workshop: Uwe Bonnes, Thomas Bickelhaupt, Roland Simon, Roland Veit
Financial Support: BMBF, DFG, GRK 2128 „AccelencE“
Thank You!