## Slide 1
WP 9.3 progress at INFN-LNL
on Nb3Sn films R&D via DCMS
Dorothea Fonnesu – INFN Legnaro National Labs
I.FAST 13th WP9 meeting
HZB Helmholtz-Zentrum Berlin – 02.12.2024

## Slide 2: Outline
Recap about last meetings (16.04.2024 IFAST WP9 Meeting Paris + 17.09.2024 Thin Films Workshop Paris)
New sputtering system with 2” magnetron
Study of film morphology
Status of samples exchange

## Slide 3: Where we left
Optimized Recipe for Nb3Sn on small samples via DCMS
4” magnetron with commercial stoichiometric single target
Low cathode power < 20 W
Deposition pressure 2 x 10-2 mbar
No annealing
Deposition temperature 600 ºC – 650 ºC
Nb buffer layer on copper substrate ≥ 30 μm
First RF test of QPR sample Nb3Sn/bulk Nb at HZB
Rs ~ 23 nΩ @ 4.5 K, 20 mT, 400 MHz
Quench > 70 mT @ 4.5 K
Tc = 17.8 K in agreement with inductive measurement
bulk

## Slide 4: New Nb3Sn sputtering system
Former V3Si system re-commissioned
all vacuum chambers cleaned
turbo molecular pump replaced
valves check and replacement
new sample holder (2 IR lamps) designed
new resistive bands for baking
2” magnetron with commercial stoichiometric Nb3Sn single target

## Slide 5: New Nb3Sn sputtering system
Validation of new system in DCMS regime
2” magnetron with commercial stoichiometric Nb3Sn single target
Depositions on Al3O2 substrate
Low cathode power < 240 mW/cm2
Deposition pressure 2 x 10-2 mbar
No annealing
Deposition temperature 650 ºC
Tc = 17.5 K 2” system operation validated and reproducibility of Nb3Sn DCMS recipe with 4” system demonstrated

## Slide 6: Morphology study
Lehrstuhl für
Oberflächen- und
Werkstofftechnologie
Courtesy of A. Zubtsovskii
Sn-rich islands observed on Nb3Sn sample surface

## Slide 7: Morphology study
Defined island parameters over inspected area:
islands count
island average perimeter
island average area
total area covered by islands
Under study dependencies from:
applied cathode power
deposition temperature
film thickness
duration of deposition process and critical temperature
[Started as Master thesis project by Matteo Lazzari]
Courtesy of M. Lazzari

## Slide 8: Travelling samples
CEA: Nb3Sn/NbBL/Cu for SC gap measurement
DESY: 2x disks Nb3Sn/NbBL/Cu; 2x Nb3Sn/bulk Nb for thermal conductivity measurement
HZB: 2x slabs Nb3Sn/NbBL/Cu and Nb3Sn/Cu for thermoelectric current measurement
HZDR: Nb3Sn/NbBL/Cu samples tbd based on last results + 6 GHz cavity (long term) for FLA
On our side:
from HZB: QPR copper sample soon to be coated at LNL
from LOT: Tc measurements ongoing at LNL

## Slide 9: Backup

## Slide 10
650

## Slide 11
Nb3Sn/Nb[50µm]/Cu at 500°C
Nb3Sn/Nb[30µm]/Cu at 600°C