## Slide 1
Institute of Electrical Engineering SAS
Eugen SEILER, (Rastislav RIES)
IFAST WP9 Meet (Berlin), 2 Dec 2024
SC characterization at IEE Bratislava

## Slide 2
IEE OVERVIEW
Uni Siegen:
● NbTiN films on Si substrate – 23.11.2023 series
STFC Daresbury:
● Nb3Sn , Nb films on Cu substrate – 12.1.2024 series
● Nb , (Nb3Sn , NbTiN) films on Cu substrate – 23.2.2024 series
Bag 1, Bag 4, Bag 5
INFN Legnaro:
● Nb3Sn films on Cu, Cu+Nb and Sapp substrates – 8.2.2024 series
Run#33, Run#36
All delivered sample batches were finalised by mid-July
After maintenance, repairs & tests (Aug-Oct), PPMS now fully operational again

## Slide 3
Table-summary

## Slide 4
Magnetization loops’ Overview & Comparison

## Slide 5
Nb3Sn / Cu,Cu+Nb,Sapp INFN (Run 33, 8.2.2024 series)
Virgin norm
Loop norm
Run 33: deposition 600°C, Nb3Sn-1μm
Nb3Sn/Nb50um/Cu
Sapphire
Cu
Sapphire sample – ‘Smash-cleaving’
Standard centering (35mm)
zoom

## Slide 6
6
Nb3Sn / Cu+Nb,Sapp INFN (Run 36, 8.2.2024 series)
Run 36: deposition 600°C, Nb3Sn-0.6μm
Nb3Sn/Nb40um/Cu
Sapphire
Nb9um/Cu
Sapphire sample – ‘Smash-cleaving’
Standard centering (35mm)
zoom
Virgin norm
Loop norm

## Slide 7
Nb3Sn/Cu , NbTiN/Cu STFC (from 23.2.2024 series)
Nb3Sn
NbTiN
Virgin norm
Loop norm
full Loops

## Slide 8
Nb / Cu STFC (from 23.2.2024 series)

## Slide 9
NbTiN / Si SiegenUni (23.11.2023 series) Bag 5 , Bag 4
Standard centering (35mm)
recentre (32mm)
full Loops
Bag 5
Bag 5
Bag 4
Bag 4

## Slide 10
Thank you for your attention