## Slide 1
Shengqiang Zhou s.zhou@hzdr.de
Semiconductor Materials
Helmholtz-Zentrum Dresden-Rossendorf (HZDR)
Semiconductor materials
processing by ion beams
for chip and quantum technologies

## Slide 2: Wolfgang Pauli
One shouldn’t work on semiconductors, that is a filthy mess; who knows if they really exist!

## Slide 3
The basic element in chips

## Slide 4
Seite 4
Ion Beam Center
Notes: 4

## Slide 5
Seite 5
Ion Beam Center at HZDR
Notes: 5

## Slide 6: Ion irradiation effect in matter
Ions flux: 108-15 ions/second, Target: 1022 atoms/cm3
large number of interactions -> questions must be answered using approximation, statistics and probabilities

## Slide 8
Ion implantation: effect

## Slide 9
Common defects in materials
Wang et al., J. Appl. Phys. 115, 17C104, (2014)
Ion implantation: effect

## Slide 10
Depth (nm)
Concentration
Diffusion
Pushing the doping limit by non-equilibrium processing
Ion implantation:
Ion species: n and p
Energy: depth
Fluence: concentration
E1 < E2 < E3
Implantation profile

## Slide 11: Isotope-selectivity!
Poate and Saadatmand, Rev. Sci. Instrum., 73, 868 (2002)

## Slide 12
Semiconductor Materials
Ion implantation works far away from thermal equilibrium, allowing us to dope semiconductors with exotic elements
up to large concentration of 1…10%. Flash lamp or pulsed laser processes materials down to milli- or nano- second time scale.
We create ultra-high doped Ge using Flash lamp annealing and ferromagnetic semiconductors using pulsed laser melting.
Different thermal processing at different time scale

## Slide 13
Helmholtz Innovation Lab:
Compound Semiconductors
Pulse duration (ms)
Energy density (Jcm-2)
0.1
1
20
10
100
1
10
Silicon
Germanium
TCO
Printed inks
Precursors
organics
roll-to-roll (R2R)
sheet-to-sheet (S2S)
 | S2S | R2R
Energy density per pulse | medium large | low
Pulse length | ms range | < 1 ms
Flash frequency | low | medium / high
# of lamps | many | one or few
Illuminated area | whole area | stripe-type part

## Slide 14
Doping and defect engineering by ions
Quantum Photonics & Optoelectronics
Semiconductors for energy and environment
Sub-second thermal processing
Semiconductor Materials

## Slide 15
Material processing: laser and flash lamp annealing
SQUID-VSM
SQUID-MPMS
Lakeshore Hall Measurement system
1.8-400 K
up to 7 T
Material characterization: magnetic and electrical
And the user facilities: ion beam center
Material characterization: optics
Raman, PL, ODMR

## Slide 16: Ion beam and sub-second annealing for materials processing
Break the doping limit
Color centers for quantum technologies

## Slide 17
Further device minimization: node down to 1 nm
Contact resistance becomes a new problem!
G. Rengo, et al., IMEC, ECS Trans. 98, 27 (2020).
Rchannel
Gate
Source contact
Drain contact
RSD
RSD
Rcontact
Rcontact

## Slide 18
New phases from non-equilibrium processing
Ion implantation and sub-second annealing
Flash lamp: milli-second
Pulsed laser: nano-second
Epitaxial layer
Ion implantation
Maximum activation at minimum redistribution !!!

## Slide 19
The electron concentration is approaching 1021 cm-3, breaking the doping limit.
No saturation even at the impurity concentration of 2.5%.
M. Wang et al, Phys. Rev. Appl. 11, 054039 (2019)
Breaks the limit!
Pushing the doping limit: deep impurities in Si

## Slide 20
M. Wang et al,
Phys. Rev. Appl. 11, 054039 (2019)
Nanoscale 14, 2826 (2022）
Determining the lattice location of impurities
Rutherford backscattering/channeling
Te-Te dimer
Si

## Slide 21: Ion beam and sub-second annealing for materials processing
Break the doping limit
Color centers for quantum technologies

## Slide 22
Wavelength (nm)
Attenuation spectrum of silica optical fibers
http://fowiki.com/b/understand-fiber-attenuation
Why telecom-wavelength single-photon emitters in silicon?
Integration with “near-zero change” of standard CMOS technology
No need for developing a new technology!

## Slide 23
Silicon
Ion implantation/irradiation
SOI wafer
Single-point defect = single-photon source (SPS)
Defect’s atomic configuration
A substitutional-substitutional carbon pair (Cs-Cs) bounded to a silicon interstitial (Sii).
Phys. Rev. Lett. 127, 196402 (2021).
Point defect centers in silicon: The so-called G center
Defect creation by radiation damage
Opt. Express 28, 26111-26121 (2020).

## Slide 24
Spectroscopic fingerprint of the G center
Suitable for fiber-based optic communication (ZPL@1278 nm)
Indistinguishable single-photons on demand (Narrow linewidth)
Quantum photonic integrated circuits (QPICs)
Point defect centers in silicon: The so-called G center
Opt. Express 28, 26111-26121 (2020)

## Slide 25
State-of-the-art: Engineering single G centers in silicon
Carbon fluence-dependent confocal 2D Photoluminescence scans
Opt. Express 28, 26111-26121 (2020)
Excitation: 637 nm
Detection: 1200-1600 nm
Scan area: 40 x 40 µm2
Diffraction-limited spots

## Slide 26
Very large-scale integration (VLSI) quantum silicon photonics
Single G center emitters at desired locations and wafer-level scalability
I - Focused ion beam (FIB) writing
II – Broad beam ion implantation
through a PMMA mask
Read out

## Slide 27: Ultimate goal of ion beam
Deterministic ion implantation with precision at atomic level!
At the target position: there is one and only one impurity

## Slide 28: Acknowledgements
n++ doping of Si, Ge: Mao Wang, Slawomir Prucnal
Color centers: Yonder Berencen, Zhen Shang, Shuyu Wen
2D materials: Slawomir Prucnal, Kaiman Lin…
Oxide films: Changan Wang, Lei Cao, Parul Pandey

## Slide 29
Quantum communication with single-photons
Quantum internet
Secure communication (Quantum Key Distribution)
Fiber-based quantum communication
A single-photon source is the gold standard
Chip- and/or fiber-based quantum communication
No-cloning theorem

## Slide 30
A silicon quantum photonic integrated circuit (QPIC)
Chip- and fiber-based quantum communication and computing
Optical link among chips via fibers
Chip B
Chip A
Link between quantum computing and quantum communication in the same framework
Notes: These QPICs can be designed to work independently of each other, but it is even more interesting to integrate them in a modular way into large-scale quantum networks, thus enabling the link between quantum computing and quantum communication in the same framework.

## Slide 31
Focused ion-beam writing of G centers in SOI chips
Chip layout
Single dot writing
(15 x 16 spots)
20 µm
2D confocal PL map
Si++, 40 keV, Rp= 60 nm
Nat Commun 13, 7683 (2022)

## Slide 32: Resource for collaboration
All stable ions from eV to MeV
for ion implantation
Nanosecond Laser
Milli-second flash lamp
Contact: Shengqiang Zhou, s.zhou@hzdr.de

## Slide 33
Pushing the doping limit: n++ Ge by flash lamp annealing
ECV: electrochemical capacitance–voltage (carrier profiling)
SIMS: secondary ion mass spectroscopy (impurity profiling)
P doped Ge films grown on Si substrates
Vohra et al. J. Appl. Phys. 125, 025701 (2019)
Prucnal et. al. New J. Phys. 22, 123037 (2020)

## Slide 34
Dissolving P4V clusters in Ge by Flash lamp annealing
Released Vacancies from P4V
join V-clusters
Kujala et al., J. Phys.: Condens. Matter 28, 335801 (2016)
Vohra et al. J. Appl. Phys. 125, 025701 (2019)
Prucnal et. al. New J. Phys. 22, 123037 (2020)

## Slide 35
2D Materials: FWIM + FWIH + FWIO + FWIN + ….
CrSBr
Nano Lett. revision

## Slide 36: CrSBr
Klein J, et al. ACS nano, 2023, 17(6): 5316-5328.
a
b
Notes: This is the optical image of CrSBr we exfoliated on SiO2.
a and b axis can be easily identified by its needlelike shape.
This is the band structure of bulk CrSBr pubilished recently.
showing a flat conduction band along the Γ−X direction, which corresponds to the a direction, and a highly dispersive band along the Γ−Y direction, which corresponds to the b direction.
The nearly flat conduction band along the Γ-X direction provides high possibility of phonon-assisted transitions.